## Slide 1
MICRO-PHOTOLUMINISCENCE FROM InAs/GaAS QUANTUM DOT MOLECULES GROWN BY DROPLET EPITAXY
G. Muñoz-Matutano1, J. Canet-Ferrer1, D. Fuster1, J. Martínez-Pastor1
P. Alonso-González2, B. Alén2, I. Fernández-Martínez2, Y. González2, F. Briones2, L. González2
1UMDO (unidad asociada al IMM-CSIC), Instituto de Ciencias de los Materiales, Universitat de València.
2IMM-CNM-CSIC: Instituto de Microelectrónica de Madrid.

## Slide 2
MICRO-PHOTOLUMINISCENCE FROM InAs/GaAs QUANTUM DOT MOLECULES GROWN BY DROPLET EPITAXY
OUTLOOK:
1. Introduction: Quantum Dot Molecule.
2. Droplet Epitaxy Growth: optical features.
3. Sample and Experimental Set-Up.
4. Lateral QD molecule results.
i) Voltage Features.
ii) Molecular Coupling.
5. Vertical QD molecule preliminar results.
6. Conclusions.

## Slide 3
1. INTRODUCTION: QD MOLECULES
Growth Direction
Growth Direction
VERTICAL MOLECULES
LATERAL MOLECULES
e-
h+
1. Electron states coupling (e- Tunneling )
2. Hole states coupling (h+ Tunneling )
3. Excitonic state couplin ( Föster copling (virtual photon))

## Slide 4
1. INTRODUCCIÓN: DEL QD AISLADO AL CRISTAL DE QDs
E.A. Stinaff et al, Science 311, 636 (2006)
H.J. Krenner et al, PRL 94, 57402 (2005)
C.J. Beirne et al, PRL 96, 137401 (2006)
VERTICAL MOLECULES
LATERAL MOLECULES
TUNNING QD STATES WITH ELECTRIC FIELD

## Slide 5
2. DROPLET EPITAXY GROWTH:
ADVANTAGES :
Localized nanostructures.
Low density samples.
Growth by QD pairs.
P. Alonso-González et al, Crystal Growth and Design 9, 2525 (2009)
L.Wang et al, New Journal of Physics 10, 045010 (2008)

## Slide 6
Density ≈ 2.5 x 108 cm-2
Negative excitonic complex.
Arsenic Vacancies.
P. Alonso-González et al, APL 91, 163104 (2007)
HIGH OPTICAL QUALITY
2. DROPLET EPITAXY GROWTH:

## Slide 7
3. SAMPLE AND EXP. SET UP: Lateral Molecules.
110
1-10
InAs Droplets Pairs.
Schottky Diode.
Field on 110
1 - 1,5 µm
Au-Cr
ΔV
E (110)
GaAs
InAs

## Slide 8
3. SAMPLE AND EXP. SET-UP: Vertical Molecules.
P. Alonso-González et al, APL 93, 183106 (2008)
First layer:
  QDs grown by Droplet Epitaxy
Second layer:
  4 nm of GaAs
Tercera capa:
  Self assembled QDs localized on first layer QDs.
1.2 ML
1.4 ML
1.6 ML

## Slide 9
3. SAMPLE AND EXP: SET-UP: Vertical Molecules.

## Slide 10
3. SAMPLE AND EXP. SET-UP: Confocal Microscope.
Laser
μPL Signal

## Slide 11
LATERAL MOLECULE
RESULTS

## Slide 12
4. RESULTS: Lateral Molecules
QDs DROPLET PAIRS: Voltage Features.
Journal of Physics: Conference Serires 210, 012015 (2010)
Type I: Isolated
Type II: Decoupled pair

## Slide 13
4. RESULTS: Lateral Molecules
QDs DROPLET PAIRS: Voltage Features.
Journal of Physics: Conference Serires 210, 012015 (2010)
Type III: Coupled pair

## Slide 14
4. RESULTS: Lateral Molecules
QDs DROPLET PAIRS: Coupling (optical signatures)
V = 5.7 V

## Slide 15
4. RESULTS: Lateral Molecules
QDs DROPLET PAIRS: Coupling
Positive Sweep
Identified some examples of anticrossing μPL evolution.
ZOOM 1
ZOOM 2

## Slide 16
VERTICAL MOLECULE RESULTS

## Slide 17
4. RESULTS: Vertical Molecules Preliminary Results
m-PL
m-PL
QD-A
QD-B
QD-C
m-PL
1.4 ML
Ensemble
QD Droplet (QD1) + SAQD (QD2)

## Slide 18
4. RESULTS: Vertical Molecules Preliminary results
E.A. Stinaff et al, Science 311, 636 (2006)
Anomalous stark shifts (Blue y Red Shifts)

## Slide 19
MICRO-PHOTOLUMINISCENCE FROM InAs/GaAs QUANTUM DOT MOLECULES GROWN BY DROPLET EPITAXY
Conclusions:
Lateral Molecules:
  Different Voltage features.
  Optical anticrossings as signatures of molecular coupling.
2. Vertical Molecules:
  Optical evidences from two different QDs.
  Anomalous QCSE shifts.